## Slide 1
measuring the resistance change of the PdNi wires due to H2-Exposure
Thin-Film-Hydrogen-Sensor Typ I
Al2O3

## Slide 2: Thin-Film-Hydrogen-Sensor
gassensitive Pd /Ni thin Film
measuring the resistance change of the PdNi thin film due to H2-Exposure
interdigital Pt-electrodes

## Slide 3
α-Phase | β-Phase
electrically conductive | semiconductive, high resistive
metallic opaque | transparent
properties of Pd alloy
depeding on H-content in the Pd-crystal lattice

## Slide 4
Halbleiter Gas-Sensor
„Elektronische Nase“

## Slide 5
Chemische Sensoren

## Slide 6
Halbleiter Gas-Sensor
„Elektronische Nase“

## Slide 8
Microscopy

## Slide 9: design of electrodes
Comb and Zig Zig Electrode structure
created by eagle software
varying width, length and distances
data file required for laser etching

## Slide 10
Structuring thin film by Lithography

## Slide 11
Lift-Off Process
Aim: Structuring metal thin films without etching!
1. Structuring photoresist (exposure, development)
2. deposition of metallic thin film (ex. Pd)
3. stripping photoresist
4. resist with metal will be removed, structured
metal on substrate remains

## Slide 12
Sputtering

## Slide 13: Sputtering PdNi alloy
to compare: coated and uncoated Alumina platles
after sputtering at 4x10-3 mbar Ar, 55 W Power, 5 min

## Slide 14
Laser structuring

## Slide 15
measuring under H2-Exposure

## Slide 16
measuring under CH4-Exposure